The following chemical cleaners are approved for service cleaning of Specialty Manufacturing, Inc. yellow polycarbonate crossing rods.

**Degreasing and Tar Removal:**

Mineral Spirits Isopropyl Alcohol VM&P Naptha

**General Cleansing:**

JetSpray Fantastik Windex

Joy Top Job Mr. Clean

Formula 409

For general protection and to facilitate easier cleaning, standard car wax may be applied as a general protectant.

**The following chemicals and cleaners should NOT be used:**

Ammonia

Simple Green

Phosphoric Acid (aluminum wheel cleaner)

Toluene

MEK

Xylene

Lacquer Thinner

Safe Fleet Bus & Rail

13501 South Ridge Drive

Charlotte, NC 28273

Toll Free: 800-951-STOP (7867)

Phone: 704-247-9300

Fax: 980-216-4606

[www.safefleet.net](http://www.safefleet.net)

For Technical Support, Email: [ncTechSupport@safefleet.net](mailto:ncTechSupport@safefleet.net)

More technical publications available at: <https://busandrail.safefleet.net/resources/technical-bulletins/>

This manual contains proprietary information of Safe Fleet. It is intended solely for the information and use of parties operating and maintaining the equipment described herein. Such proprietary information may not be used, reproduced, or disclosed to any other parties for any other purpose without the expressed written permission of Safe Fleet. Controlled copies of Safe Fleet documents are maintained within Safe Fleet. Printed or electronic copies in other storage locations are uncontrolled.